ROYAL INDUSTRIAL SUPPLIERS

GST NO.: 29AHZPU5620Q1ZZ

An ISO 9001:2015 Certified Company

QUALITY FASTENERS SPECIALIST

8310165941 / 9959457863	sales@royalfastenersindia.com        www.royalfastenersindia.com

TECHNICAL DATA SHEET

SELF CLINCHING NUT (CLS)

MATERIAL- STAINLESS STEEL

GRADE-SS304 (A2)

AS PER-NON-STANDARD

CATALOGUE NO. R4S15

INSTALLATION GUIDE

- VERIFY THE NUT SIZE, THREAD TYPE, AND MATERIAL MATCH THE APPLICATION REQUIREMENT.

- ENSURE THE BASE MATERIAL IS DUCTILE AND SUITABLE FOR SELF CLINCHING INSTALLATION.

- PUNCH OR DRILL THE MOUNTING HOLE TO THE SPECIFIED DIAMETER AND TOLERANCE.

- CONFIRM THE HOLE IS ROUND, CLEAN, AND FREE FROM BURRS OR CONTAMINATION.

- INSERT THE SELF CLINCHING NUT INTO THE HOLE FROM THE CORRECT INSTALLATION SIDE.

- ENSURE THE NUT HEAD OR FLANGE IS FLUSH AGAINST THE BASE MATERIAL SURFACE.

- USE A FLAT, PARALLEL PRESS TOOL OR HYDRAULIC PRESS FOR INSTALLATION.

- APPLY STEADY, AXIAL PRESS FORCE WITHOUT ROTATION.

- ALLOW THE BASE MATERIAL TO FLOW INTO THE NUT’S UNDERCUT GROOVE.

- DO NOT HAMMER OR APPLY IMPACT FORCE DURING INSTALLATION.

- VERIFY THE NUT IS FULLY SEATED AND FLUSH WITH THE MATERIAL SURFACE.

- CHECK THAT THE NUT DOES NOT SPIN OR PULL OUT AFTER INSTALLATION.

- AVOID OVER-PRESSING TO PREVENT PANEL DISTORTION OR THREAD DAMAGE.

- ENSURE THREADS ARE CLEAR AND UNDAMAGED AFTER INSTALLATION.

- INSPECT THE FINAL ASSEMBLY FOR ALIGNMENT, HOLDING STRENGTH, AND SURFACE FLATNESS.

| Dimension↓ Size→ | Tol | M2x0.4 | M2.5x0.45 | M3x0.5 | M3.5x0.6 | M4x0.7 | M5x0.8 | M6x1.0 | M8x1.25 | M10x1.5 | M12x1.25 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Collar dia d2 | max | 4.22 | 4.22 | 4.22 | 4.73 | 5.38 | 6.38 | 8.72 | 10.47 | 13.97 | 16.95 |
| Nut dia d3 | ±0.25 | 6.25 | 6.35 | 6.35 | 7.10 | 7.87 | 8.64 | 11.18 | 12.70 | 17.35 | 20.57 |
| Nut thickness m | ±0.25 | 1.50 | 1.50 | 1.50 | 1.50 | 2.00 | 2.00 | 4.08 | 5.47 | 7.48 | 8.50 |
| Hole Size in Sheet | +0.08 | 4.25 | 4.25 | 4.25 | 4.75 | 5.40 | 6.40 | 8.75 | 10.50 | 14.00 | 17.00 |
| Minimum edge distance to hole centre |  | 4.80 | 4.80 | 4.80 | 5.60 | 6.90 | 7.10 | 8.60 | 9.70 | 13.50 | 16.00 |

Quote the PART NUMBER given below with your order/ inquiries:     	        All Dimensions in mm

| Size | Shank Code | Item Code | Min Sheet Thickness sm | h (Shank) Max | Press In KN |  | Push out N |  | Torque out Nm |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Aluminium | Steel | Aluminium | Steel | Aluminium | Steel |
| M2x0.4 | 0 | R4S1502000 | 0.80 | 0.77 | 6.7 - 8.9 | 11.2 - 15.6 | 280 | 470 | 0.90 | 1.47 |
|  | 1 | R4S1502001 | 1.00 | 0.97 |  |  | 400 | 550 | 1.13 | 1.70 |
|  | 2 | R4S1502002 | 1.40 | 1.38 |  |  | 750 | 980 | 1.47 | 1.90 |
| M2.5x0.45 | 0 | R4S1520500 | 0.80 | 0.77 | 6.7 - 8.9 | 11.2 - 15.6 | 280 | 470 | 0.90 | 1.47 |
|  | 1 | R4S1520501 | 1.00 | 0.97 |  |  | 400 | 550 | 1.13 | 1.70 |
|  | 2 | R4S1520502 | 1.40 | 1.38 |  |  | 750 | 1010 | 1.47 | 1.90 |
| M3x0.5 | 0 | R4S1503000 | 0.80 | 0.77 | 6.7 - 8.9 | 11.2 - 15.6 | 280 | 470 | 0.90 | 1.47 |
|  | 1 | R4S1503001 | 1.00 | 0.97 |  |  | 400 | 550 | 1.13 | 1.70 |
|  | 2 | R4S1503002 | 1.40 | 1.38 |  |  | 600 | 900 | 1.47 | 1.90 |
|  | 3 | R4S1503003 | 2.30 | 2.21 |  |  | 700 | 1010 | 1.55 | 2.00 |
| M3.5x0.6 | 0 | R4S1530500 | 0.80 | 0.77 | 11.2 - 13.4 | 13 - 26 | 280 | 490 | 1.80 | 2.30 |
|  | 1 | R4S1530501 | 1.00 | 0.97 |  |  | 400 | 570 | 2.30 | 2.71 |
|  | 2 | R4S1530502 | 1.40 | 1.38 |  |  | 800 | 1080 | 2.60 | 3.20 |
| M4x0.7 | 0 | R4S1504000 | 0.80 | 0.77 | 11.2 - 13.4 | 18 - 27 | 300 | 490 | 2.37 | 2.95 |
|  | 1 | R4S1504001 | 1.00 | 0.97 |  |  | 470 | 645 | 2.60 | 3.80 |
|  | 2 | R4S1504002 | 1.40 | 1.38 |  |  | 970 | 1250 | 4.00 | 4.20 |
|  | 3 | R4S1504003 | 2.30 | 2.21 |  |  | 1000 | 1300 | 4.10 | 4.50 |
| M5x0.8 | 0 | R4S1505000 | 0.80 | 0.77 | 11.2 - 15.6 | 18 - 38 | 300 | 530 | 3.00 | 3.60 |
|  | 1 | R4S1505001 | 1.00 | 0.97 |  |  | 480 | 800 | 3.60 | 4.50 |
|  | 2 | R4S1505002 | 1.40 | 1.38 |  |  | 845 | 1112 | 5.70 | 5.80 |
|  | 3 | R4S1505003 | 2.30 | 2.21 |  |  | 880 | 1200 | 5.70 | 6.80 |
| M6x1.0 | 0 | R4S1506000 | 1.20 | 1.15 | 11.2 - 13.4 | 27 - 36 | 970 | 1380 | 7.90 | 13.00 |
|  | 1 | R4S1506001 | 1.40 | 1.38 |  |  | 1540 | 1680 | 10.20 | 16.00 |
|  | 2 | R4S1506002 | 2.30 | 2.21 |  |  | 1600 | 1750 | 13.50 | 16.80 |
|  | 3 | R4S1506003 | 2.30 | 2.21 |  |  | 1680 | 1850 | 14.10 | 18.50 |
| M8x1.25 | 1 | R4S1508001 | 1.40 | 1.38 | 11.2 - 15.6 | 27 - 36 | 1570 | 1870 | 13.60 | 18.70 |
|  | 2 | R4S1508002 | 2.30 | 2.21 |  |  | 1720 | 1980 | 18.10 | 19.30 |
| M10x1.5 | 1 | R4S1510001 | 2.31 | 2.21 | 18 - 32 | 32 - 50 | 1680 | 1900 | 30.70 | 32.50 |
|  | 2 | R4S1510002 | 3.18 | 3.05 |  |  | 1800 | 2020 | 34.20 | 38.00 |
| M12x1.75 | 1 | R4S1512001 | 3.18 | 3.05 | 28 - 40 | 42 - 67 | 1980 | 4250 | 38.50 | 79.50 |

Sizes in BLUE are non-preferred. Availability is limited and MOQ is applied       Data is strictly informative