ROYAL INDUSTRIAL SUPPLIERS

GST NO.: 29AHZPU5620Q1ZZ

An ISO 9001:2015 Certified Company

QUALITY FASTENERS SPECIALIST

8310165941 / 9959457863	sales@royalfastenersindia.com        www.royalfastenersindia.com

TECHNICAL DATA SHEET

SELF CLINCHING THROUGH HOLE STANDOFF (SOS)

MATERIAL- STAINLESS STEEL

GRADE-SS304 (A2)

AS PER-NON-STANDARD

CATALOGUE NO. R4S19

INSTALLATION GUIDE

- VERIFY THE STANDOFF SIZE, LENGTH, THREAD TYPE, AND MATERIAL MATCH THE APPLICATION REQUIREMENT.

- ENSURE THE BASE MATERIAL IS DUCTILE AND SUITABLE FOR SELF CLINCHING INSTALLATION.

- PUNCH OR DRILL THE MOUNTING HOLE TO THE SPECIFIED DIAMETER AND TOLERANCE.

- CONFIRM THE HOLE IS ROUND, CLEAN, AND FREE FROM BURRS OR CONTAMINATION.

- INSERT THE SELF CLINCHING STANDOFF INTO THE HOLE FROM THE SPECIFIED INSTALLATION SIDE.

- ENSURE THE STANDOFF HEAD IS FLUSH AGAINST THE BASE MATERIAL SURFACE BEFORE    PRESSING.

- USE A FLAT, PARALLEL PRESS TOOL OR HYDRAULIC PRESS FOR INSTALLATION.

- APPLY STEADY, AXIAL PRESS FORCE WITHOUT ROTATION.

- ALLOW THE BASE MATERIAL TO FLOW INTO THE STANDOFF’S UNDERCUT GROOVE.

- DO NOT HAMMER OR APPLY IMPACT FORCE DURING INSTALLATION.

- VERIFY THE STANDOFF SHOULDER IS FULLY SEATED AND FLUSH WITH THE MATERIAL           SURFACE.

- CHECK THAT THE THROUGH HOLE IS CLEAR AND FREE FROM DISTORTION.

- CONFIRM THE STANDOFF DOES NOT SPIN OR PULL OUT AFTER INSTALLATION.

- AVOID OVER-PRESSING TO PREVENT PANEL DISTORTION OR STANDOFF DAMAGE.

- INSPECT THE FINAL ASSEMBLY FOR ALIGNMENT, HOLDING STRENGTH, AND SURFACE FLATNESS.

| Size |  | M2x0.4 | M2.5x0.45 | M3x0.5 | 3.5M3x0.5 | M3.5x0.6 | M4x0 .7 | M5x0.8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C -0.13 |  | 4.20 | 4.20 | 4.20 | 5.39 | 5.39 | 7.12 | 7.12 |
| H nom |  | 4.80 | 4.80 | 4.80 | 6.40 | 6.40 | 7.90 | 7.90 |
| Counter bore dia B ±0.13 |  | 3.20 | 3.20 | 3.20 | 3.20 | 3.90 | 4.80 | 5.35 |
| Hole Size in Sheet +0.08 |  | 4.22 | 4.22 | 4.22 | 5.41 | 5.41 | 7.14 | 7.14 |
| Min sheet thickness |  | 1.02 | 1.02 | 1.02 | 1.02 | 1.02 | 1.27 | 1.27 |
| Min Dist. Hole C/L to edge |  | 6.00 | 6.00 | 6.00 | 6.80 | 6.80 | 8.00 | 8.00 |
| Max tightening torque for mating screw Nm |  | 0.20 | 0.20 | 0.40 | 0.40 | 0.70 | 1.40 | 2.60 |
| Installation KN | 5052-H34 AL | 4.80 | 4.80 | 4.80 | 7.50 | 7.50 | 10.60 | 10.60 |
|  | Cold Rolled Sheet | 9.60 | 9.60 | 9.60 | 14.50 | 14.50 | 17.60 | 17.60 |
| Pushout N | 5052-H34 AL | 700 | 700 | 700 | 1300 | 1300 | 1750 | 1750 |
|  | Cold Rolled Sheet | 1000 | 1000 | 1000 | 1860 | 1860 | 2480 | 2480 |
| Torque Out NM | 5052-H34 AL | 1.02 | 1.02 | 1.24 | 1.24 | 2.82 | 5.08 | 5.08 |
|  | Cold Rolled Sheet | 1.95 | 1.95 | 2.15 | 2.15 | 3.90 | 8.40 | 8.40 |

Quote the PART NUMBER given below with your order/ inquiries:     	        All Dimensions in mm

| D ±0.5 | Dia→ Length↓ | M2x0.4 | M2.5x0.45 | M3x0.5 | 3.5M3x0.5 | M3.5x0.6 | M4x0 .7 | M5x0.8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 3 | R4S1902003 | R4S1920503 | R4S1903003 | R4S1903103 |  | R4S1904003 |  |
|  | 4 | R4S1902004 | R4S1920504 | R4S1903004 | R4S1903104 | R4S1930504 | R4S1904004 | R4S1905004 |
|  | 5 | R4S1902005 | R4S1920505 | R4S1903005 | R4S1903105 | R4S1930505 | R4S1904005 | R4S1905005 |
|  | 6 | R4S1902006 | R4S1920506 | R4S1903006 | R4S1903106 | R4S1930506 | R4S1904006 | R4S1905006 |
|  | 8 | R4S1902008 | R4S1920508 | R4S1903008 | R4S1903108 | R4S1930508 | R4S1904008 | R4S1905008 |
| 4.00 | 10 | R4S1902010 | R4S1920510 | R4S1903010 | R4S1903110 | R4S1930510 | R4S1904010 | R4S1905010 |
|  | 12 | R4S1902012 | R4S1920512 | R4S1903012 | R4S1903112 | R4S1930512 | R4S1904012 | R4S1905012 |
|  | 14 | R4S1902014 | R4S1920514 | R4S1903014 | R4S1903114 | R4S1930514 | R4S1904014 | R4S1905014 |
| 8.00 | 16 | R4S1902016 | R4S1920516 | R4S1903016 | R4S1903116 | R4S1930516 | R4S1904016 | R4S1905016 |
|  | 18 |  |  | R4S1903018 | R4S1903118 | R4S1930518 | R4S1904018 | R4S1905018 |
|  | 20 |  |  | R4S1903020 | R4S1903120 | R4S1930520 | R4S1904020 | R4S1905020 |
| 11.00 | 22 |  |  | R4S1903022 | R4S1903122 | R4S1930522 | R4S1904022 | R4S1905022 |
|  | 25 |  |  | R4S1903025 | R4S1903125 | R4S1930525 | R4S1904025 | R4S1905025 |
|  | 30 |  |  | R4S1903030 | R4S1903130 | R4S1930530 | R4S1904030 | R4S1905030 |
|  | 35 |  |  | R4S1903035 | R4S1903135 | R4S1930535 | R4S1904035 | R4S1905035 |
|  | 40 |  |  | R4S1903040 | R4S1903140 | R4S1930540 | R4S1904040 | R4S1905040 |
|  |  | Length Tolerance +0.05 -0.13 |  |  |  |  |  |  |

Sizes in BLUE are non-preferred. Availability is limited and MOQ is applied       Data is strictly informative